## Slide 1
Saudi Basic Corporation (SABIC)
Presented By: Manabendra Maity
YOUR LOGO
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
Reliable refractory lining design to prevent acid dew point corrosion in process fired heaters and furnaces

## Slide 2
AGENDA
Introduction- process fired Heaters and Furnaces
Concluding remarks
Q&A
Importance of Refractories
Acid Dew Point Condensation & Reactions in furnaces
Effects of Acidic condensation: Risks & challenges
Preventive safeguards: Refractory design & operation

## Slide 3
Abstract:
Fired heaters and furnaces are amongst the most essential and expensive assets in hydrocarbon process industries including refineries, petrochemicals, fertilizers, and allied plants. These process equipment items are heart of the hydrocarbon industries as majority of processes and productions are directly dependent on the performances of the above equipment items. Refractory materials are used in heaters and furnaces as thermal insulation and provide necessary protection to the furnace structure against thermal, mechanical and chemical stresses.
Fuels used in these assets often contain sulfurous compounds and other impurities of varying quantities. The sulfur in the fuel could combine with the oxygen in the air during combustion to form sulfur dioxide (SO2) and sulfur trioxide (SO3). Flue gases originating from combustion of sulphur containing fuels can combine with water can condense into sulfuric acid (H2SO4), sulfurous acid (H2SO3), and other aggressive constituents below acid dew-point temperature of flue gas mixes. Therefore, flue gas components can easily penetrate the porous refractory to the steel shell behind the refractory layers. If the shell temperature is below the acid dew point of the gas, acidic condensation will occur. The corrosive flue gases and acid condensates will potentially corrode the internal metallic casing, supports, refractory linings in the radiant and convection sections, flue gas ducts, stacks, and air preheater thus resulting in severe damage to the assets. Acid vapors and condensates typically deteriorate the refractory integrity and functional properties. In case of metal, dew point corrosion typically results in excessive metal loss, leading to perforation or rupture. The onset of deterioration cannot be easily identified because these regions and surfaces are covered with refractory and not usually accessible for visual inspection. Unidentified damage mechanisms in a furnace refractory and casing can result in catastrophic equipment failures, unplanned shutdowns, and high maintenance costs.
Adequacy of a refractory system against potential dew point condensation and associated damage mechanisms is often given little consideration during refractory design and material selection. The extent of the dew point corrosion and its effect could be reduced by careful selection of refractory material, lining design system and thermal gradients and operational controls. This paper will highlight the fundamental acid dew point corrosion issues and associated risks encountered in fired heaters and similar assets with case studies. In addition, it will address common protective design measures and techniques to avoid corrosion problems.
Key words: Heater, Refractory, Lining, dew-point, Corrosion.
RELIABLE REFRACTORY LINING DESIGN TO PREVENT ACID DEW POINT CORROSION IN PROCESS FIRED HEATERS AND FURNACES

## Slide 4
FIRED HEATERS & REFRACTORY LININGS

## Slide 5
Process fired heaters and furnaces
Fired Heater: (op. temp.~600 to 11500C)
Olefin / Ethylene / Cracking Furnace (~12000C).
Steam (Primary) Reformer (~12000C).
  Methanol,
  Ammonia,
  Hydrogen,
  Syn Gas (GTL, DRI), etc.
Operating Temperature ~ 700 – 12000C
Fuels: Gas & Oil
Operating atmosphere: Oxidizing,
Operating pressure: slightly -ve
Casing/ Shell Temperature ~ 60 - 1000C
Thermal Efficiency > 90%
Typical operating parameters
Heaters & Furnaces (Gas / Oil Fuel)
Heaters & Furnaces
Radiant Section
Convection
Section
Air Preheater
Hot Flue Gas Duct
Cold Flue Gas Duct
Alternative Stack
Stack

## Slide 6
Radiant Tubes
Outside 60-1000C
Inside 11500C
Heat Radiation from wall
Essential materials for high temperature assets
Refractory plays multiple roles:
  Structural Thermal Protection
  Heat Insulation & reduce losses
  Corrosion / Erosion Protection, etc.
Refractory performance & service life control
  EHSS Risks
  Integrity & Reliability of assets
  Plant Availability
  Production & Product quality
  Plant Economics
  Sustainability…
Refractory insulation reduces
  Fuel consumption
  CO2 & NOx emissions
Refractory Importance
Temperature Gradient
Steel Plate
Refractory Layers
Refractory Lining Types
Refractory Layers
Refractory Importance
Refractory Hot Face
Refractory lining
Steel Casing Temp: 60-1000C

## Slide 7
Heater REFRACTORY PERFORMANCE & Failure risks
      Important features
        Large-scale production : Big size with high production capacity.
        Plants continuously operated for 2-5 years without shutdown
        Single stream operation: Usually No back-up or spare equipment/ furnaces ;
        Plants and equipment are integrated- failure of any heater may cause total shutdown
      Refractory failures and non-performances lead to
        Hot spots, Shell overheating, structural degradation.
        Loss of containment and associated RISKS.
        Unsafe operating conditions: EHSS Risks.
        High thermal energy losses .
        Reduced efficiency / production load.
        Unplanned downtime - production losses.
        High maintenance costs…….etc.
+600ºC
Refractory failure & Hot spot
Furnace casing plate –ruptured

## Slide 8
FLUE-GAS DEW POINT
&
ACIDIC CONDENSATION

## Slide 9
Flue gas acid dew point condensation
Oil
Gas: Natural gases, Process off & waste gases, sour natural gas, sour refinery gas,
Impurities in Fuels
Fuels contain acidic compounds (e.g., Sulfur, Cl)
Oil (S ~ 0.3 to 5.0%)
Gas ( H2S in PPM level)
Combustion of S-containing fuels produces flue gases that contain acid gases ( HCl, SOX ) and water vapor.
Flue gas constituents:
CO2 , CO, N2 (Gases)
H2O (Steam),
SO2 & SO3 , NOx , Cl (Gases)
Compounds of Na, V, Ash etc.
Fuel Combustion > 5000 C
Fuel combustion:
CH4 + O2  CO2 + H2O (Steam) + N2 + NOx (gas)
Impurities  SO2 , SO3, Cl.. (gaseous / vapor constituents):
Fuels used in Heaters & furnaces
Dew Point (Td ): Dew point is the temperature at which the first liquid starts to condense from the gas phase.
When flue gas temperature drops below a certain temperature, acidic gases and water vapor condense to form Acids (H2SO4, H2SO3, H2CO3, HNO3, HCl)
Flue Gas Acid Dew Point (FGADP) Condensation in Heaters
Fuel / Air elements | Combustion Yields -gases | Condensates / Acidic Compounds | FGADP temperatures
H2 | H2O (steam) | H2O (water) | FGADP temperatures increase as concentration of gas phases increases Example: S concentrations of 5 to 5000 ppm typically produce FGADP temperatures of approx. 90°C to 150°C. Source: API 560:Fired Heaters For General Refinery Service
C | CO and CO2 | H2CO3 | 
S | SO2 & SO3 | H2SO4 / H2SO3 | 
N2 | NO & NO2 | HNO3 | 
Cl | Cl2 & HCl | HCl | 

## Slide 10
S + O2 SO2 (Gas)
(Conversion ~ 1-5 %)
SO2 + O2 SO3 (Gas)
H2 SO4 (Gas)
H2 SO4 (Liquid)
Gas Phase
Typical dew point temperature:
H2SO4 Sulphuric acid: 150°C to 175°C.
HNO3 Nitric acid: 40°C to 65°C.
HCl Hydrochloric acid: 50°C to 68°C.
(H2O, SOX, NOx , Cl)
Flue gas Acid dew point (FGADP) condensation
< Dew Point
Temperature
FGADP Condensation typically happen during Operation, Start-up & Shut-down at locations/ regions inside heater where temperature fall below dew points.
Acids may condense onto the walls and refractory.
Cause severe & rapid corrosion of steel structures, anchors & refractory.
Acid formation in Heaters
+ H2O (Steam)
Fuel Combustion

## Slide 11
PREFRACTORY LINING : PRACTICAL ISSUES
Porous material (Bricks, Castable, Ceramic Fibre, Insulating Board)
  Porosity ~ 10 to + 90%
  High Permeability
  Gas permeation from hot face to cold face.
Flue gas channeling / leakage through lining Joints, Cracks & Gaps
Heaters design and operated for High Thermal Efficiency > 90%
High Thermal insulation: Reduce shell temperature & heat losses.
  Reduced shell temp. (60 - 1000C) potentially led to more condensation.
  In cold ambient condition, shell temp. can drop below dew point.
Maximum heat recovery from flue gas: Reduced flue gas temperature-
  Overcooling of acidic flue gas may result in condensation.
  Risk of acid condensation at downstream components (ducts, chimney)
  If (flue gas wetted) cold-end metal temperatures were allowed to decline below the sulfuric acid dew point temperature, it would be possible for a system to experience the corrosion.
Refractory materials & lining : practical issues
High thermal efficiency and associated risks
Castable + Brick Weight
>750 kg/m3
Ceramic Fiber Weight
128- 220 kg/m3
Refractory wall
Temperature Gradient
Steel Casing Temp: 60-1000C
Refractory Hot Face
Gap/ joint
Gap/ joint
Radiant Section
Convection
Section
Air Preheater
Hot Flue Gas Duct
Cold Flue Gas Duct
Alternative Stack
Stack

## Slide 12
DEW POINT ACIDIC CONDENSATION: RISKS & CHALLENGES

## Slide 13
Dew point ACIDIC CONDENSATION and associated problems
Refractory materials: Main Oxides : Al2O3 , SiO2 , CaO, MgO, Cr2O3, ZrO2,..Other Impurities: Fe2O3, Na2O, K2O, etc.
Refractory-Acid Chemical reaction:
    Formation of sulphates (Sulphating) in wet H2SO4 environments.
    Destructive reaction with Basic / alkali refractory oxides (e.g., CaO  CaSO4).
    Deteriorated refractory characteristics & reduced life.
Castable and concrete: Degradation of the cement-binding phases.
    Calcium aluminate (Cao- Al2O3 cement) bonded refractories : H2SO4 and CaO compounds reacts.
    Typically form calcium sulfate (CaSO4)2H2O, a growth salt.
    Subsequent hydration of CaSO4 causes an expansion within the matrix, which further degrades refractory.
Mortar- binders: tend to have problems in wet H2SO4 environments.
    Alkali- silicate bonded mortar (Sodium / Potassium silicate) forms complexes sulfate compounds.
    Examples: Formation of sodium sulphate hydrates: (NaSO4)2 .H2O, Na2SO4 .10H2O.
    These salts crystallize & expand volumetrically: Cause cracking and spalling of refractory.
    Acidic condensation & absorption within porous refractory:
    Increased thermal conductivity of refractory & increased heat losses.
    Swelling & weakening of structure….. (e.g., Calcium Silicate insulating block).
Refractory materials and linings degradations in wet H2SO4 environments
Insulating Block / Concrete
Refractory Brick
Anchor
(Steel)
Temp: 60-1000C
Steel Plate
Steel Casing
Brick joint
binder/mortar
Steel Plate
Refractory Linings & components
Temperature Gradient
Refractory Hot Face
Temp: 60-1000C

## Slide 14
Corrosion & Anchor weld detached
Shell
Anchor / shell corrosion: Brick-wall detached & tilted
Wide Gap: Shell & Brick-wall
Condensation of sulfur containing acids on steel parts.
Corrosion of steel casing , metallic anchors & support.
  Thinning of casing plate and perforation.
  Reduced structural integrity.
  Anchor failures lead to lining failure.
  Perforation in casing plate resulting in leakage of hot gases.
Dew point ACIDIC CONDENSATION and associated problems
Corrosion of Furnace steel casing , anchors & support Structures
Acidic condensation- refractory fallen (Flue gas duct)
Refractory collapsed due to thinning of shell plate
Casing Thinning & perforation
Outside- Steel casing/ Shell corroded /leaked
Steel plate thinning & perforation
Hole in Steel Casing

## Slide 15
After Service: Acidic condensation and deposition on steel surface
New plate - lining
Corrosion: Anchor base & shell plate
Dew point ACIDIC CONDENSATION: CORROSION ON STEEL & REFRACTORY
Stack- Chimney : Steel Severely corroded

## Slide 16
ACIDIC CONDENSATION: RISKS & CHALLENGES (CUR- CORROSION UNDER REFRACTORY)
A hidden deterioration of both refractory and steel structure.
Acidic Condensation & CUR can be widespread or localized.
Stacks and Cold flue gas ducts are susceptible to rapid deterioration when temperature drops below dew point.
Inspection and prevention of CUR is a difficult task.
Generally, not accessible for visual examination of refractory and casing.
Onset of corrosion cannot be easily identified.
Often, significant time passes before taking the initiative to inspect refractory and structure.
Refractory condition, left unchecked, could cause serious impact on reliability, availability and maintenance cost.

## Slide 17
REFRACTORY DESIGN MEASURES & PREVENTIVE SAFEGUARDS

## Slide 18
identify FG adp condensation possibilities and risks
Review following issues / questions:
  Identify Fuel impurities, if any (acidic components?)
  Which condensed liquid/ Acid can be formed?
  Which amount of condensed liquid can be expected?
  What concentration of corrosive liquid can be expected?
  What is the corrosion resistance of the material in expected environment?
Measurement of Flue Gas Acid Dew Point Temperature: acidic gasses SO3, SO2, Cl and NOX
  API 560 (Fired Heaters For General Refinery Service): Guidelines for calculation

## Slide 19
Refractory design Measures to prevent acid Dew point corrosion
API 560 recommends a limit of 10 mg/kg of sulfur content in fuel for corrosion protection requirement.
800C
Steel Shell
Refractory Thickness
Dew Point
Td
Barrier : SS Foil
Paint / Membrane Coating on steel casing (internal):
  High temperature acid resistant paint /coating
  Fuels sulfur content > 10 mg/kg (10 ppm by mass)
Ceramic Coating:
  Impervious coating on refractory hot surface to reduce permeation of gas.
Barrier : SS Foil
Barrier : SS Foil
Vapor Retarders / Physical Barrier to acid gas permeation:
  Impermeable gastight membrane or barrier embedded between refractory layers.
  Barrier prevent permeation of acidic gases towards cold refractory face & casing...........
  Typically, a thin metallic Foil / Sheet (0.1 to 0.2mm) : SS or aluminum is used.
  Barrier placed in lining at temperature above the dew point of gases.
Mastic coating on casing
Barrier : SS Foil

## Slide 20
Refractory design Measures to prevent acid Dew point corrosion
External
insulation
Inner Shell
Outer
cladding
Refractory + External system
Steel Casing wall temperature control to reduce condensation:
  Maintain high steel casing temperature (above dew point) using a less internal insulation.
  Disadvantage: Higher energy loss.
External Insulation : Refractory + External insulation:
  Reduce heat losses & maintain high steel casing temperature.
  Suitable for regions / components operate at relatively low temperature / at colder locations.
  Examples: Flue gas duct, stack.
  Concern: Possible overheating & corrosion on metal casing.
Refractory
Temperature Gradient

## Slide 21
Refractory design Measures to prevent acid Dew point corrosion
Acid resistant refractory materials
  Install corrosion resistant proprietary materials.
  Refractory with high silica and less alkalis & impurities, such as CaO, MgO, Fe2O3, Na2O, K2O, etc.
  Hot face: Use relatively dense & impervious refractories to reduce permeation.
  Back-up refractory:
    Should be non-soluble in presence condensates / water.
    Use of calcium silicate block should be avoided.
  Flue gas duct, chimney (colder locations): Use acid resistant special insulating castable & bricks and mortars.

## Slide 22
Operation & inspection practices
Operational control:
  Effective control on Sulphur content in fuel by regularly monitoring and maintaining it as per design conditions
  Maintain a higher flue gas exhaust temperature above dew point (say +150C) .
  Injection of Special additives to reduce conversion of SO2 to SO3 .
Inspection & maintenance practices:
Establish appropriate inspection strategy for vulnerable components considering both risks of condensation and internal corrosion.
Steel shell /casing plate:
  Thickness measurement (e.g., UT) of casing plate can check for corrosion and thickness loss.
  Most susceptible locations / components can be closely inspected & monitored.
  Visual inspection for leakage.
Refractory
  Best way to inspect for CUR is to remove the refractory lining locally.
  However, this can be time consuming, costly and not practical in many cases.
  Involve experienced SMEs having practical experiences.

## Slide 23
Concluding remarks
FGADP Corrosion under refractory (CUR) is hidden deterioration of both refractory and steel structure.
Inspection- assessment and prevention of FGADP Corrosion is a difficult task.
Risks can be reduced, if flue gas ingress and / or condensation on steel casing and into refractory system are eliminated / reduced.
Various controllable variables influence the CUR:
  Identify hidden risks associated with acidic condensations.
  Safeguards: Refractory design, material, coating, casing temperature controls, operational controls, etc.
  Combining different materials in a properly designed and installed system affords the required protection.
  Ensure management of change (MOC) procedure if there is a plan to change fuel that might have high of S- contaminant.
  Establish appropriate inspection strategy for locations considering both risks of condensation and internal corrosion damage.

## Slide 24
Reach out.
THANK YOU
maitym@sabic.com
+966 530702835
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
YOUR LOGO