## Slide 1: Rehabilitation of Business- Critical Seawater Cooling Tower
confidential
Wasim Idris Baig
Abdulrahman Al-Shahrani
Projects Engineering Department -Cathodic Protection
Syed Shams Shiraz,
SABIC Agri-Nutrients

## Slide 2: contents
Introduction
Background
Condition Assessment
Installation of Scaffolding
CP System Design and Installation
CP System Performance Assessment
Significance of Cathodically Protecting Critical Assets
confidential

## Slide 3: introduction

## Slide 4: introduction
confidential
Cylindrical/ conical shape Reinforced Concrete Seawater Cooling Towers (CT) operate in very harsh environments that can cause severe corrosion, deterioration and spalling of concrete.
The spalling of concrete pieces from above pose an EHSS concern for personnel working around the CT.
If the structure loses it integrity due to the severe damages it can pose as business risk if the CT underwent shutdown.
Carrying out repair of these structures is very challenging and expensive due to its height, geometry and getting an access on the structure during operations.

## Slide 5: background
Rehabilitation of EHSS/ Business Critical Seawater Cooling Tower

## Slide 6: background
confidential
The Cooling Tower (CT) was built in 2006
Cylindrical/ conical in shape and consists of 24 fans around the circumference used for cooling the hot seawater.
The height of the CT is 52m, the diameters at the bottom and top are 72.6m and 53.3m respectively.
The thicknesses of the CT shell at the bottom and top are 600mm and 200 mm respectively.
Cathodic Protection (CP) system was provided up to 14m of shell portion for the internal reinforcement only.
Top 10 meters of external surface of the CT were coated with epoxy-based coating.

## Slide 7: Condition assessment

## Slide 8: Visual assessment

## Slide 9: SEVERE CORROSION OF STEEL REINFORCEMENT AND DELAMINATION OF CONCRETE

## Slide 10: Fan supports

## Slide 11: External Fan rings

## Slide 12: Scaffolding installation

## Slide 13: Scaffolding installation

## Slide 14: SCAFFOLDING PLAN WITH ONE ANCHOR BOLT

## Slide 15: Temporary repair carried out at severe damaged areas to fix scaffolding

## Slide 16: Scaffolding platform

## Slide 17: CP System design
Cp design

## Slide 18: Cp design- walkway

## Slide 19: Cp design- ct shell

## Slide 20: CP design Fan supports

## Slide 21: cP design Shell lower level and fan rings

## Slide 22: Cp system installation

## Slide 23: Surface preparation

## Slide 24: Debris management

## Slide 25: Anode installation

## Slide 26: Typical CP system installation with scaffolding supports in place
Competencies
Skills
Knowledge

## Slide 27: Mmo Anode mesh installation arrangement for wind ribs

## Slide 28: CP system installation, shotcrete and coating

## Slide 29: Significance of Cathodically Protecting Critical Assets
Section divider subtitle

## Slide 30: Significance of Cathodically Protecting Critical Assets
Corrosion of steel in concrete is critical, and if left unaddressed it can lead to catastrophic failures and safety risk to living beings.
Plants have large reinforced concrete seawater reservoirs which provide cooling system to the plants. Hence, integrity of these structures is very critical to the plant operations.
Complete shutdown of the complex can happen if the cooling tower goes out of service due to structural integrity.
Difficult to repair damaged Concrete structures in congested areas.
The corrosion of reinforcing steel is considered one of the major cause of deterioration of steel reinforced concrete structures. Applying Cathodic Protection from initial stages can prevent expensive mitigation measures, prevent unplanned turnarounds and save huge costs.

## Slide 31: Rust is must
Mighty ships upon the ocean Suffer from severe corrosion,
Even those that stay at dockside Are rapidly becoming oxide
Alas that piling in the sea is mostly Fe2O3,
And where the ocean meets the shore You’ll find there’s Fe3O4,
Because when the wind is salt and gusty
Things are getting awful rusty.
We can measure we can test it,
We can halt it or arrest it,
We can gather it and weigh it,
We can coat it, we can spray it,
We examine and dissect it,
We Cathodically protect it,
We can pick it up and drop it,
So here’s to rust, no doubt about it,
Most of us would starve without it.
T.R.B Watson, June 1974

## Slide 32
Thank you
Notes: To select different Thank You options, go to HOME tab and click Layout button.